## Slide 1: Analysis of Poisson Ratio Data in Piezo Actuator Stacks
BY: Winnie Wang, undergraduate
Quantum Material Labs, University of Washington

## Slide 2: What’s the Poisson Ratio? Why is it important?

## Slide 3: Background
“Piezo-stack”: A highly incompressible material
  Stretches very minimally under low temperatures
Poisson Ratio (“ν”): (Ratio of transverse strain):(ratio of axial strain)
  Transverse = compressed; axial = tensile
Potentially useful for data analysis and comparison
  Strain measurement experiments
  Replace unstable data

## Slide 4: Background
Ratio of compressed and tensile strains
  Tensile (‘T’) and compressed (‘C’) direction
  ‘GF’ = gauge factor
  ‘SG’ = strain gauge
  ‘ε’ =strain

## Slide 5: Experimental Set-up
Piezo stack is glued with varnish on a small metal bar
Two strain gauges are glued with “stycast” onto the piezo-stack
The whole setup is then put in a cryostat
  Piezo-stack is ramped with different voltages to induce change in resistance

## Slide 6: 1st Setup
2nd Setup
0-130V
2 strain gauges
Piceramic
-40-40V
1 Cross Strain Gauge
Piezomechanik

## Slide 7: 1st Setup
2nd Setup

## Slide 8: 1st Setup

## Slide 9: 2nd Setup

## Slide 10: Measurement Procedure
Poisson Ratios are analyzed from 2 piezo-stacks
  Piceramic (Jan. 2017) and Piezomechanik (Mar. 2017)
Experiment starts at 300K
  Goes down to 0K and back up at a regular temp. interval
  System waits for about 200 seconds at each T (for equilibrium)
Voltage is ramped through the piezo-stack
  A hysteresis graph is obtained at each temperature
Process repeats at the next temperature

## Slide 11: Measurement Procedure
Data analysis process:
  Best fit of all hysteresis is done at each temperature range
    To obtain the average strain/volt at each temperature range
  The fitted strain/volt at each temperature is then plotted
    Poisson ratio is calculated from each fitted data point

## Slide 12: Results

## Slide 20: Discussion
New material (Piezomechanik) displayed poorer quality results
  Than compared to one done in January (Piceramic)
Potential reasons:
  Small voltage range?
  Not enough stycast?
  Different material?

## Slide 21: Thank you for listening!